SECTION 09720 (09 72 16.16)

HYGIENIC WALL CLADDING

FOR BEHAVIORAL MENTAL HEALTH

GENERAL

SECTION INCLUDES

Hygienic wall coverings. (Altro Whiterock) (Altro Whiterock Chameleon) (Altro Whiterock Digiclad High Quality Graphic Printed) (Altro Whiterock Matte) (Altro Whiterock Wall Designs)

Accessories:  Behavioral and mental health facilities. (Altro Whiterock) (Altro Whiterock Chameleon) (Altro Whiterock Digiclad High Quality Graphic Printed) (Altro Whiterock Matte) (Altro Whiterock Wall Designs)

RELATED SECTIONS

Section 03300 - Cast-in-Place Concrete.

Section 06100 - Rough Carpentry: Sheathing.

Division 7 - Thermal and Moisture Protection.

Division 15 - Mechanical.

REFERENCES

ASTM International (ASTM):

ASTM E 84 Standard Test Method for Surface Burning Characteristics of Building Materials. Class A.

ASTM D 5420 - Standard Test Method for Impact Resistance of Flat, Rigid Plastic Specimen by Means of a Striker Impacted by a Falling Weight (Gardner Impact).

Underwriters Laboratories of Canada (ULC):

CAN/ULC-S102, Surface Burning Characteristics.

SUBMITTALS

Submit under provisions of Section 01300 - Administrative Requirements.

Product Data:  Manufacturer's data sheets on each product to be used, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

Shop Drawings:

Selection Samples:  For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.

Verification Samples:  For each finish product specified, two samples, minimum size 6 inches (152 mm) square representing actual product, color, and patterns.

QUALITY ASSURANCE

Manufacturer Qualifications: Minimum 5 year experience manufacturing similar products.

Installer Qualifications:  Trained journeymen with a minimum of three years successful experience in the installation of wall coverings.

Mock-Up: Provide a mock-up for evaluation of surface preparation techniques and application workmanship.

Finish areas designated by Architect.

Do not proceed with remaining work until workmanship is approved by Architect.

Remodel mock-up area as required to produce acceptable work.

PRE-INSTALLATION MEETINGS

Convene minimum two weeks prior to starting work of this section.

DELIVERY, STORAGE, AND HANDLING

Deliver and store products in manufacturer's unopened packaging bearing the brand name and manufacturer's identification until ready for installation.

Store rolls of sheet goods in a secured upright position. Store materials in dry spaces protected from the weather, with ambient temperatures not less than 55 degrees F (12.8 degrees C) or more than 85 degrees F (29.4 degrees C).

Handle materials to avoid damage.

PROJECT CONDITIONS

Temperature Requirements: If storage temperature is below 65 degrees F (18 degrees C), the Altro Whiterock wall panel must be moved to a warmer place and allowed to reach this temperature before installation. For further information, refer to current Installation Guide.

Maintain air temperature and structural base temperature at installation area between 65 degrees F (18 degrees C) and 80 degrees F (26 degrees C) for 48 hours before, during and 24 hours after installation.

SEQUENCING

Ensure that products of this section are supplied to affected trades in time to prevent interruption of construction progress.

WARRANTY

Warranty:  Provide manufacturer’s standard limited warranty.

EXTRA MATERIALS

Provide extra materials of product and adhesives in accordance with submittal requirements as specified in Division 1.

Material of each color, pattern and type required for maintenance use from same production run as installed materials.

Quantity (sq ft/sq m):  ______.

Clearly identify each wall panel and each container of adhesive.

PRODUCTS

MANUFACTURERS

Acceptable Manufacturer:  Altro USA, Inc., which is located at:  80 Industrial Way, Wilmington, MA 01887; ASD Toll Free Tel:  800-377-5597; Tel:  978-657-6464; Fax:  610-746-4325; Email: Support@altrofloors.com; www.altro.com.

Substitutions: Not permitted.

Requests for substitutions will be considered in accordance with provisions of Section 01600 - Product Requirements.

HYGENIC WALL COVERINGS

Basis of Design:  Altro Whiterock, as manufactured by Altro USA Inc. 100 percent pure vinyl, extruded, semi-rigid PVCu sheet containing no plasticizers or fillers. Altro Whiterock is homogenous.

Impact resistance per ASTM D5420:  160 in-lbs (18.1 N-m).

Surface Burning Characteristics Compliance: CAN/ULC-S102 and ASTM E84.

Thickness:  0.100 in (2.5 mm).

Thickness:  0.125 in (3 mm).

Panel Dimensions (WxH):  48 x 98.42 in (1219 x 2500 mm).

Weight:  23.59 lbs (10.7 kg).

Panel Dimensions (WxH):  48 x 118.11 in (1219 x 3000 mm).

Weight:  28.22 lbs (12.8 kg).

Product Identification:  Standard White W103 (2.5m) / W104 (3m).

Product Identification:  Cream / Linen W136/41 (2.5m) / W137/41 (3m)

Product Identification:  Champagne / Oyster W136/32 (2.5m) / W137/32 (3m).

Product Identification:  Praline / Fenland W136/219 (2.5m) / W137/219 (3m).

Product Identification:  Sage / Promenade W136/212 (2.5m) / W137/212 (3m).

Product Identification:  Lagoon / Flint W136/201 (2.5m) / W137/201 (3m).

Product Identification:  Snowdrift / Ice W136/44 (2.5m) / W137/44 (3m).

Product Identification:  Sapling / Seafoam W136/43 (2.5m) / W137/43 (3m).

Product Identification:  Jasmine / Cesco W136/53 (2.5m) / W137/53 (3m).

Product Identification:  Ghost / Echo W136/208 (2.5m) / W137/208 (3m).

Product Identification:  Platinum / Urban W136/210 (2.5m) / W137/210 (3m).

Product Identification:  Mocha / Fawn W136/206 (2.5m) / W137/206 (3m).

Product Identification: Bergamot: W136/220 (2.5m) / W137/220 (3m).

Product Identification: Mint W136/203 (2.5m) / W137/203 (3m).

Product Identification: Olea W136/218 (2.5m) / W137/218 (3m).

Product Identification: Ozone W136/211 (2.5m) / W137/211 (3m).

Product Identification: Scarlett W136/221 (2.5m) / W137/221 (3m).

Product Identification: Vibrance W136/213 (2.5m) / W137/213 (3m).

Product Identification: Zandra W136/217 (2.5m) / W137/217 (3m).

Product Identification: Viola (W136/214 (2.5m) / W137/214 (3m).

Product Identification:  As indicated on the Drawings.

Product Identification:  As selected by Architect.

Accessories:  For behavioral and mental health facilities.

Joint Strips:  1-Part-G831/25 white. 98.5 in (2502 mm) length.

Joint Strips:  1-Part-G831/30 white. 118 in (2997 mm) length.

Altro Weld Rod:  WSR01; white.

Altro Weld Rod:  WSR. Color determined by Architect from manufacturer’s selection.

Basis of Design:  Altro Whiterock Chameleon, as manufactured by Altro USA Incorporated. 100 percent pure vinyl, extruded, semi-rigid PVCu sheet containing no plasticizers or fillers. Altro Whiterock Chameleon is homogenous.

Surface Burning Characteristics Compliance: CAN/ULC-S102 and ASTM E84.

Thickness:  0.100 in (2.5 mm).

Panel Dimensions (WxH):  48 x 98.42 in (1219 x 2500 mm).

Weight:  22.93 lbs (10.4 kg).

Panel Dimensions (WxH):  48 x 118.11 in (1219 x 3000 mm).

Weight:  28.00 lbs (12.7 kg).

Product Identification:  Distant Thunder 6634.

Product Identification:  Eau De Chic 6605.

Product Identification:  Slip Stream 6611.

Product Identification:  Feng Shui 6617.

Product Identification:  Taxi Cab 6636.

Product Identification:  Shocking Pink 6616.

Product Identification:  Moulin Rouge 6618.

Product Identification:  Night Fall 6622.

Product Identification:  Liquorice 6612.

Product Identification:  Pure Innocence 6601.

Product Identification:  Sheer Glass 6609.

Product Identification:  Hawaiian Palm 6638.

Product Identification:  Juicy Lucy 6620.

Accessories:  For behavioral and mental health facilities.

Joint Strips:  1-Part-G831/25 white. 98.5 in (2502 mm) length.

Joint Strips:  1-Part-G831/30 white. 118 in (2997 mm) length.

Altro Weld Rod:  WSR01; white.

Altro Weld Rod:  WSR. Color determined by Architect from manufacturer’s selection.

Basis of Design: Altro Whiterock Digiclad High Quality Graphic Printed, as manufactured by Altro USA Incorporated. 100 percent pure vinyl, extruded, semi-rigid PVCu sheet containing no plasticizers or fillers. Hard coat protective layer is added to prevent damage to the graphics.

Surface Burning Characteristics Compliance: CAN/ULC-S102 and ASTM E84.

Impact resistance per ASTM D5420:  160 in-lbs (18.1 N-m).

Thickness:  0.100 in (2.5 mm).

Panel Dimensions (WxH):  48 x 98.42 in (1219 x 2500 mm).

Weight:  23.59 lbs (10.7 kg).

Panel Dimensions (WxH):  48 x 118.11 in (1219 x 3000 mm).

Weight:  28.22 lbs (12.8 kg).

Accessories: For behavioral or mental health facility.

Altro Weld Rod:  WSR01; white.

Altro Weld Rod:  WSR. Color determined by Architect from manufacturer’s selection.

Basis of Design: Altro Whiterock Matte, as manufactured by Altro USA Inc. 100 percent pure vinyl, extruded, semi-rigid PVCu sheet containing no plasticizers or fillers. Altro Whiterock Matte is homogenous.

Impact resistance per ASTM D5420:  160 in-lbs (18.1 N-m).

Surface Burning Characteristics Compliance: CAN/ULC-S102 and ASTM E84.

Thickness:  0.125 in (3 mm).

Panel Dimensions (WxH):  48 x 98.42 in (1219 x 2500 mm).

Weight:  23.59 lbs (10.7 kg).

Panel Dimensions (WxH):  48 x 118.11 in (1219 x 3000 mm).

Weight:  28.22 lbs (12.8 kg).

Product Identification: Pearl FT41.

Product Identification: Battleship FT208.

Product Identification: Tan FT206.

Product Identification: Almond FT32.

Product Identification:  As indicated on the Drawings.

Product Identification:  As selected by Architect.

Accessories:  For behavioral and mental health facilities.

Joint Strips:  1-Part-G831/25 white. 98.5 in (2502 mm) length.

Joint Strips:  1-Part-G831/30 white. 118 in (2997 mm) length.

Altro Weld Rod:  WSR01; white.

Altro Weld Rod:  WSR. Color determined by Architect from manufacturer’s selection.

Basis of Design: Altro Whiterock Wall Designs High Quality Graphic Printed, as manufactured by Altro USA Incorporated. 100 percent pure vinyl, extruded, semi-rigid PVCu sheet containing no plasticizers or fillers. Hard coat protective layer is added to prevent damage to the graphics.

Surface Burning Characteristics Compliance: CAN/ULC-S102 and ASTM E84.

Impact resistance per ASTM D5420:  160 in-lbs (18.1 N-m).

Thickness:  0.100 in (2.5 mm).

Panel Dimensions (WxH):  48 x 98.42 in (1219 x 2500 mm).

Weight:  23.59 lbs (10.7 kg).

Panel Dimensions (WxH):  48 x 118.11 in (1219 x 3000 mm).

Weight:  28.22 lbs (12.8 kg).

Product Identification: Metallic / Brushed Steel / 9911 / WDS259911 (8’ panel) / WDS309911 (10’ panel) / 54 LRV.

Product Identification: Metallic / Antique Copper / 9912 / WDS259912 (8’ panel) / WDS309912 (10’ panel) / 10 LRV.

Product Identification: Concrete / White Mineral / 9905 / WDS259905 (8’ panel) / WDS309905 (10’ panel) / 61 LRV.

Product Identification: Concrete / Cool Mineral / 9906 / WDS259906 (8’ panel) / WDS309906 (10’ panel) / 48 LRV.

Product Identification: Concrete / Urban Mineral / 9907 / WDS259907 (8’ panel) / WDS309907 (10’ panel) / 28 LRV.

Product Identification: Linen / Winter Weave / 9909 / WDS259909 (8’ panel) / WDS309909 (10’ panel) / 58 LRV.

Product Identification: Linen / Autumn Weave / 9910 / WDS259910 (8’ panel) / WDS309910 (10’ panel) / 43 LRV.

Product Identification: Linen / Summer Weave / 9908 / WDS259908 (8’ panel) / WDS309908 (10’ panel) / 36 LRV.

Product Identification: Wood / Soft Woodgrain / 9901 / WDS259901 (8’ panel) / WDS309901 (10’ panel) / 52 LRV.

Product Identification: Wood / Warm Woodgrain / 9904 / WDS259904 (8’ panel) / WDS309904 (10’ panel) / 38 LRV.

Product Identification: Wood / Smoky Woodgrain / 9903 / WDS259903 (8’ panel) / WDS309903 (10’ panel) / 19 LRV.

Product Identification: Wood / Rich Woodgrain / 9902 / WDS259902 (8’ panel) / WDS309902 (10’ panel) / 14 LRV.

Accessories:  For behavioral or mental health facility.

Altro Weld Rod:  WSR01; white.

Altro Weld Rod:  WSR. Color determined by Architect from manufacturer’s selection.

EXECUTION

EXAMINATION

Do not begin installation until substrates have been properly prepared.

If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

PREPARATION

Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

Walls: Smooth and level. High points removed and low points filled with filler intended for the substrate and environmental conditions.

Wall tiles:  Firmly to the wall. As long as the tile edges do not protrude you do not have to skim grout joints.

Surfaces:  Permanently dry and free from substances that may contribute to adhesive bond failure.

Remove loose paint and conduct an adhesive bond test with paint.

Exterior walls:  Adequately damp-proofed and insulated.

Dry Wall Substrates:  Paint ready.

Absorbent and porous substrates must have a proprietary sealer minimum of 12 hours prior to the installation.

Electrical switches, power points etc., should be in a first fix installation state.

Fitting to Door Frames: In place prior to installation wall covering.

Complete painting in contact with wall covering. Sealant used at junctions is non-paintable.

Clean surfaces thoroughly prior to installation.

INSTALLATION

Install in accordance with manufacturer's instructions, approved submittals, and in proper relationship with adjacent materials.

All Seams shall be heat welded with Altro Weldrod only.

For Behavioral and Mental Health Facilities:

Joining Method, Adjacent Floor and Wall Materials:

Rebate installation method.

Pencil cove installation method

Do not us weldrods to adjoin wall panels to flooring when using the rebate installation method or pencil cove installation method.

Joining Method, Wall Panels to Each Other. Weldrod installation method is acceptable

Coved Installation: Where Altro flooring is coved up wall surfaces and other abutments, install per Altro Installation Practices using the following accessories:

Standard Wall Finishes:  Rebate method. Firmly secure sheet vinyl beneath wall panel prior to sealing with security sealant.

Shower Transitions:  Pencil cove method. With wall flush against flooring. Ensure there are no opportunities to pick at finishes by installing Altro Whiterock wall cladding over flooring per this installation method.

PROTECTION

Protect installed products until completion of project.

Cleaning:  Remove temporary coverings and protection of adjacent work areas. Repair or replace damaged installed products. Clean installed products in accordance with manufacturer’s instructions prior to Owner’s acceptance. Remove construction debris from project site and legally dispose of debris.

Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION